| ILLUSTRATED REPORT FOR BRILLIANT |  |  | Parameter | Avg | Min | Max | Dev | Cut | Sym |  |  | 1 | 2 | 3 | 4 | 5 | 6 | 7 | 8 |
| --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- |
| Polished Brilliant |  |  |  | Diameter, mm | 5.821 | 5.817 | 5.826 | 0.14% | E | EX |  |  | 5.822 | 5.821 | 5.820 | 5.819 |  |  |  |  |
|  |  |  |  | Crown angle, ° | 34.55 | 34.38 | 34.71 | 0.33 | Grading | EX |  |  | 34.51 | 34.38 | 34.40 | 34.58 | 34.63 | 34.71 | 34.62 | 34.55 |
|  |  |  |  | Pavilion angle, ° | 40.73 | 40.60 | 40.94 | 0.34 | Grading | EX |  |  | 40.78 | 40.94 | 40.87 | 40.75 | 40.67 | 40.60 | 40.60 | 40.67 |
| Model | Simple |  |  | Total height, % | 60.64 |  |  |  | E |  |  |  |  |  |  |  |  |  |  |  |
| Expert name | Makoed A.G. |  |  | Crown height, % | 14.68 | 14.52 | 14.77 | 0.25 | E | EX |  |  | 14.52 | 14.60 | 14.63 | 14.76 | 14.77 | 14.75 | 14.71 | 14.68 |
| Report date | 07.03.2008 |  |  | Pavilion depth, % | 42.93 | 42.73 | 43.16 | 0.43 | N/A | EX |  |  | 43.11 | 43.16 | 43.00 | 42.82 | 42.77 | 42.73 | 42.85 | 42.97 |
| Real weight, ct |  |  |  | Table, % | 57.36 | 57.22 | 57.47 | 0.25 | Grading | EX |  |  | 57.47 | 57.42 | 57.34 | 57.22 |  |  |  |  |
| Calculated weight, ct | 0.73, 0.7286 |  |  | Culet, % | 0.36 | 0.32 | 0.39 | 0.07 | E | EX |  |  |  |  |  |  |  |  |  |  |
| Measurements | 5.821 (5.817-5.826) x 3.530 /0.004 mm |  |  | Girdle Bezel, % | 3.04 | 2.88 | 3.16 | 0.28 | E | EX |  |  | 3.00 | 2.88 | 3.03 | 3.06 | 3.10 | 3.16 | 3.07 | 2.99 |
| Spread | 0.00 ct, 0.08% |  |  | Girdle Bone, % | 2.94 | 2.85 | 3.03 | 0.18 |  | EX |  |  | 2.95 | 2.86 | 2.85 | 2.89 | 3.03 | 2.99 | 2.98 | 3.01 |
| AGS Spread | N/A ct, N/A% |  |  | Girdle Valley, % | 1.32 | 1.20 | 1.42 | 0.22 | E | EX |  |  | 1.40 | 1.20 | 1.25 | 1.24 | 1.32 | 1.24 | 1.32 | 1.33 |
|  |  |  |  |  |  |  |  |  |  |  |  |  | 1.36 | 1.35 | 1.42 | 1.34 | 1.36 | 1.32 | 1.33 | 1.33 |
| Average values, mm |  |  | Star: | 55.99: | 55.42: | 56.68: | 1.26 | E | EX |  |  | 56.23: | 55.49: | 55.97: | 55.83: | 55.87: | 56.41: | 56.68: | 55.42: |
|  |  |  | Upper ratio, % | 44.01 | 44.58 | 43.32 |  |  |  |  |  | 43.77 | 44.51 | 44.03 | 44.17 | 44.13 | 43.59 | 43.32 | 44.58 |
| Diam | Total height | Crown height | Pav. depth | Table | Culet | Girdle |  |  | Star angle, ° | 22.81 | 22.57 | 23.05 | 0.48 |  | EX |  |  | 22.83 | 22.57 | 22.86 | 22.90 | 22.71 | 22.94 | 23.05 | 22.64 |
|  |  |  |  |  |  | Bezel | Bone | Valley |  |  | Upper girdle angle, ° | 42.39 | 42.04 | 42.76 | 0.73 |  | EX |  |  | 42.31 | 42.32 | 42.26 | 42.11 | 42.26 | 42.32 | 42.49 | 42.56 |
| 5.821 | 3.530 | 0.854 | 2.499 | 3.339 | 0.021 | 0.177 | 0.171 | 0.077 |  |  |  |  |  |  |  |  |  |  |  | 42.04 | 42.40 | 42.56 | 42.76 | 42.61 | 42.64 | 42.20 | 42.37 |
|  |  |  |  |  |  |  |  |  |  |  | Length girdle facet, % | 79.83 | 78.81 | 80.53 | 1.71 | E | EX |  |  | 80.07 | 79.32 | 79.16 | 79.52 | 79.27 | 80.18 | 78.81 | 79.71 |
|  |  |  |  |  |  |  |  |  |  |  |  | 79.71 | 80.43 | 80.45 | 80.25 | 80.53 | 79.87 | 80.15 | 79.92 |
|  |  |  | Lower girdle angle / Halves angle, ° | 41.82 | 41.65 | 42.02 | 0.38 |  | EX |  |  | 41.86 | 42.00 | 42.02 | 41.98 | 41.93 | 41.90 | 41.83 | 41.78 |
|  |  |  |  |  |  |  |  |  |  |  |  | 41.80 | 41.74 | 41.65 | 41.66 | 41.70 | 41.72 | 41.78 | 41.84 |
|  |  |  | Twist, ° | 0.23 | 0.04 | 0.43 | 0.39 |  | EX |  |  | 0.28 | 0.08 | 0.23 | 0.43 | 0.04 | 0.25 | 0.18 | 0.35 |
|  |  |  | Crown height, mm | 0.854 | 0.845 | 0.860 | 0.015 | E | EX |  |  | 0.845 | 0.850 | 0.851 | 0.859 | 0.860 | 0.858 | 0.857 | 0.854 |
|  |  |  | Pavilion depth, mm | 2.499 | 2.487 | 2.512 | 0.025 | N/A | EX |  |  | 2.509 | 2.512 | 2.503 | 2.492 | 2.490 | 2.487 | 2.494 | 2.501 |
|  |  |  | Table, mm | 3.339 | 3.331 | 3.345 | 0.015 | Grading | EX |  |  | 3.345 | 3.342 | 3.338 | 3.331 |  |  |  |  |
|  |  |  | Culet, mm | 0.021 | 0.018 | 0.023 | 0.004 | E | EX |  |  |  |  |  |  |  |  |  |  |
|  |  |  | Girdle Bezel, mm | 0.177 | 0.167 | 0.184 | 0.016 | E | EX |  |  | 0.175 | 0.167 | 0.176 | 0.178 | 0.180 | 0.184 | 0.179 | 0.174 |
|  |  |  | Girdle Bone, mm | 0.171 | 0.166 | 0.176 | 0.010 |  | EX |  |  | 0.171 | 0.167 | 0.166 | 0.168 | 0.176 | 0.174 | 0.173 | 0.175 |
|  |  |  | Girdle Valley, mm | 0.077 | 0.070 | 0.082 | 0.013 | E | EX |  |  | 0.082 | 0.070 | 0.073 | 0.072 | 0.077 | 0.072 | 0.077 | 0.077 |
|  |  |  |  |  |  |  |  |  |  |  |  | 0.079 | 0.079 | 0.082 | 0.078 | 0.079 | 0.077 | 0.077 | 0.078 |
|  |  |  | Measurement as per OctoNus theory: |  |  |  |
|  |  |  | Crown angle, ° | 34.55 | 34.51 | 34.57 | 0.06 |  |  |  |  | 34.57 | 34.55 | 34.51 | 34.57 |  |  |  |  |
|  |  |  | Pavilion angle, ° | 40.73 | 40.71 | 40.77 | 0.06 |  |  |  |  | 40.72 | 40.77 | 40.73 | 40.71 |  |  |  |  |
|  |  |  | Fish eye effect, ° | 7.73 | N/A |  |  |  | Extra Facet / Nat | No |
|  |  |  | Culet through Crown Bezel, ° | 11.66 | N/A |  |  |  | Girdle to MIC, mm | 0.004 |
|  |  |  | Parameter, ° | 1 | 2 | 3 | 4 | 5 | 6 | 7 | 8 |  |  | Paint / Dug | Avg | Type | Sym | Dev | Sym |
|  |  |  | Pav. azimuths dev. from ideal | 0.00 | -0.00 | -0.15 | -0.33 | -0.07 | 0.04 | 0.02 | 0.02 |  |  | Crown, ° | 0.20 |  | EX | 0.72 | EX |
|  |  |  | Crown azimuths dev. from ideal | -0.28 | 0.07 | 0.08 | 0.11 | -0.02 | 0.29 | 0.20 | -0.33 |  |  | Crown, notch. | 0.1, Negligible |  |  | 0.2 |  |
|  |  |  | Crown painting | 0.57 | -0.04 | 0.52 | -0.24 | 0.72 | 0.05 | 0.35 | 0.44 |  |  | Pavilion, ° | 0.02 |  | EX | 0.40 | EX |
|  |  |  |  | -0.28 | 0.15 | 0.06 | 0.54 | 0.02 | 0.05 | 0.12 | 0.09 |  |  | Pavilion, notch. | 0.0, Negligible |  |  | 0.1 |  |
|  |  |  | Pavilion painting | -0.03 | -0.14 | -0.12 | -0.18 | 0.17 | 0.05 | 0.30 | 0.14 |  |  |  |
|  |  |  |  | 0.26 | 0.40 | -0.03 | -0.18 | 0.10 | -0.00 | -0.12 | -0.32 |  |  |  |
| Appraiser title | GIA_PCTG_StarCul |  |  |  |  |  |  |  |
| Overall cut quality | E |  |  |  |  |  |  |  |
| Symmetry appraiser title | Internal |  |  |  |  |  |  |  |
| Overall symmetry quality | EX |  |  |  |  |  |  |  |
| Color |  |  |  |  |  |  |  |  |
| Clarity |  |  |  |  |  |  |  |  |
|  |  |  |  |  |  | Girdle center |  | Culet center |  | Тable center |  |  |  |
| Polish |  |  |  | Offset by table axis |  |  |  |
|  |  |  |  | Girdle-Culet | 0.14 ± 0.22, % | 0.008 ± 0.013, mm |  |  |  |
| Fluorescence |  |  |  | Girdle-Table | 0.16 ± 0.20, % | 0.009 ± 0.011, mm |  |  |  |
|  |  |  |  | Table-Culet | 0.24 ± 0.23, % | 0.014 ± 0.014, mm |  |  | Girdle to table-culet line offset | 0.11 %, 0.007 mm |