| DIAMCALC ILLUSTRATED REPORT |  |  | Parameter | Avg | Min | Max | Dev | Cut | Sym |  |  | 1 | 2 | 3 | 4 | 5 | 6 | 7 | 8 |
| --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- |
| Polished Brilliant |  |  |  | Diameter, mm | 4.778 | 4.765 | 4.792 | 0.57% | N/A | EX |  |  | 4.785 | 4.774 | 4.777 | 4.777 |  |  |  |  |
|  |  |  |  | Crown angle, ° | 32.25 | 31.11 | 32.55 | 1.44 | N/A | VG |  |  | 32.50 | 32.51 | 32.16 | 31.11 | 32.45 | 32.24 | 32.47 | 32.55 |
|  |  |  |  | Pavilion angle, ° | 40.68 | 39.68 | 41.53 | 1.86 | N/A | VG |  |  | 40.38 | 40.33 | 39.68 | 40.18 | 40.78 | 41.43 | 41.53 | 41.10 |
| Model | Sample Helium Brilliant |  |  | Total height, % | 56.96 |  |  |  | N/A | - |  |  |  |  |  |  |  |  |  |  |
| Expert name | Sample Expert Name |  |  | Crown height, % | 11.38 | 10.61 | 12.35 | 1.75 | N/A | VG |  |  | 12.35 | 12.15 | 11.58 | 10.84 | 10.67 | 10.61 | 11.15 | 11.66 |
| Report date | 06.09.2006 |  |  | Pavilion depth, % | 42.72 | 41.72 | 43.77 | 2.05 | N/A | GD |  |  | 41.72 | 42.30 | 41.99 | 42.92 | 43.60 | 43.77 | 43.17 | 42.28 |
| Real weight, ct | 0.37 |  |  | Table, % | 64.03 | 63.82 | 64.12 | 0.29 | N/A | EX |  |  | 64.06 | 64.11 | 64.12 | 63.82 |  |  |  |  |
| Calculated weight, ct | 0.37, 0.3764 |  |  | Culet, % | 0.57 | 0.39 | 0.68 | 0.28 | 0 | EX |  |  |  |  |  |  |  |  |  |  |
| Measurements, mm | 4.778 (4.765-4.792) x 2.722 /0.019 |  |  | Girdle Bezel, % | 2.84 | 2.41 | 3.40 | 0.98 | 0 | EX |  |  | 2.87 | 2.41 | 3.40 | 3.16 | 2.71 | 2.50 | 2.62 | 3.06 |
| Spread | 0.03 ct, 8.44% |  |  | Girdle Bone, % | 3.31 | 3.02 | 3.71 | 0.69 | - | EX |  |  | 3.04 | 3.55 | 3.45 | 3.08 | 3.71 | 3.04 | 3.60 | 3.02 |
|  |  |  |  | Girdle Valley, % | 1.55 | 1.22 | 1.98 | 0.75 | 0 | EX |  |  | 1.43 | 1.25 | 1.41 | 1.96 | 1.98 | 1.75 | 1.68 | 1.35 |
| Average values, mm |  |  |  |  |  |  |  |  |  |  |  | 1.64 | 1.33 | 1.31 | 1.22 | 1.42 | 1.73 | 1.71 | 1.55 |
|  |  |  | Star: | 58.29: | 53.81: | 62.79: | 8.98 | - | - |  |  | 54.81: | 58.07: | 60.72: | 58.81: | 62.79: | 59.87: | 57.44: | 53.81: |
| Total height | Crown height | Pavilion depth | Table | Culet | Girdle |  |  | Upper ratio, % | 41.71 | 46.19 | 37.21 |  |  |  |  |  | 45.19 | 41.93 | 39.28 | 41.19 | 37.21 | 40.13 | 42.56 | 46.19 |
|  |  |  |  |  | Bezel | Bone | Valley |  |  | Star angle, ° | 18.74 | 17.50 | 19.77 | 2.27 |  | GD |  |  | 19.29 | 19.45 | 19.17 | 18.52 | 17.50 | 18.26 | 17.98 | 19.77 |
| 2.722 | 0.544 | 2.041 | 3.059 | 0.027 | 0.136 | 0.158 | 0.074 |  |  | Upper girdle angle, ° | 39.95 | 39.01 | 41.04 | 2.03 | - | GD |  |  | 39.61 | 39.33 | 39.61 | 40.40 | 40.20 | 39.76 | 39.34 | 40.04 |
|  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  | 40.92 | 39.01 | 41.04 | 40.15 | 40.97 | 39.58 | 39.40 | 39.88 |
|  |  |  | Lower girdle angle / Halves angle, ° | 41.57 | 40.59 | 42.49 | 1.90 | - | VG |  |  | 41.13 | 41.12 | 41.08 | 40.59 | 40.64 | 41.00 | 41.35 | 41.58 |
|  |  |  |  |  |  |  |  |  |  |  |  | 41.83 | 42.28 | 42.44 | 42.49 | 42.29 | 42.07 | 41.84 | 41.40 |
|  |  |  | Twist, ° | 1.49 | 0.17 | 3.62 | 3.45 | - | VG |  |  | 0.40 | 0.61 | 0.58 | 2.20 | 3.62 | 0.91 | 0.17 | 3.44 |
|  |  |  | Crown height, mm | 0.544 | 0.507 | 0.590 | 0.083 | - | - |  |  | 0.590 | 0.581 | 0.553 | 0.518 | 0.510 | 0.507 | 0.533 | 0.557 |
|  |  |  | Pavilion depth, mm | 2.041 | 1.993 | 2.091 | 0.098 | - | - |  |  | 1.993 | 2.021 | 2.006 | 2.051 | 2.083 | 2.091 | 2.063 | 2.020 |
|  |  |  | Table, mm | 3.059 | 3.050 | 3.064 | 0.014 | - | - |  |  | 3.061 | 3.063 | 3.064 | 3.050 |  |  |  |  |
|  |  |  | Culet, mm | 0.027 | 0.019 | 0.032 | 0.014 | - | - |  |  |  |  |  |  |  |  |  |  |
|  |  |  | Girdle Bezel, mm | 0.136 | 0.115 | 0.162 | 0.047 | - | - |  |  | 0.137 | 0.115 | 0.162 | 0.151 | 0.129 | 0.120 | 0.125 | 0.146 |
|  |  |  | Girdle Bone, mm | 0.158 | 0.144 | 0.177 | 0.033 | - | - |  |  | 0.145 | 0.170 | 0.165 | 0.147 | 0.177 | 0.145 | 0.172 | 0.144 |
|  |  |  | Girdle Valley, mm | 0.074 | 0.058 | 0.094 | 0.036 | - | - |  |  | 0.069 | 0.060 | 0.067 | 0.094 | 0.094 | 0.084 | 0.080 | 0.064 |
|  |  |  |  |  |  |  |  |  |  |  |  | 0.078 | 0.064 | 0.062 | 0.058 | 0.068 | 0.083 | 0.082 | 0.074 |
|  |  |  | Measurement as per OctoNus theory: |  |  |  |
|  |  |  | Crown angle, ° | 32.25 | 31.83 | 32.48 | 0.65 | - | - |  |  | 32.48 | 32.38 | 32.31 | 31.83 |  |  |  |  |
|  |  |  | Pavilion angle, ° | 40.68 | 40.58 | 40.88 | 0.30 | - | - |  |  | 40.58 | 40.88 | 40.60 | 40.64 |  |  |  |  |
|  |  |  | Fish eye effect, ° | 3.62 | N/A | - |  |  | Extra Facet / Nat | Yes (2) |
|  |  |  | Culet through Crown Bezel, ° | 25.18 | N/A | - |  |  | Girdle to MIC, mm | 0.019 |
|  |  |  | Parameter, ° | 1 | 2 | 3 | 4 | 5 | 6 | 7 | 8 |  |  |  |
|  |  |  | Pav. azimuths deviation from ideal | 0.00 | 0.55 | 0.58 | 2.11 | 1.66 | 0.72 | 0.62 | 0.04 |  |  |  |
|  |  |  | Crown azimuths deviation from ideal | 0.40 | 1.17 | 0.00 | -0.09 | -1.96 | 1.63 | 0.45 | 3.48 |  |  |  |
|  |  |  | Crown painting | -1.40 | -1.47 | -2.12 | -0.51 | -1.20 | -1.17 | -0.84 | -2.94 |  |  |  |
|  |  |  |  | -1.44 | -4.13 | -0.84 | -2.95 | -0.38 | -2.04 | -1.58 | -0.43 |  |  |  |
|  |  |  | Pavilion painting | 0.21 | -1.92 | -1.49 | -0.59 | 0.92 | -0.04 | 0.09 | -0.36 |  |  |  |
|  |  |  |  | 0.11 | -1.25 | 0.96 | -0.40 | -0.07 | -0.69 | 0.19 | -0.19 |  |  |  |
| Appraiser title | AGS_2005 |  |  |  |  |  |  |  |
| Overall cut quality | 3 |  |  |  |  |  |  |  |
| Overall symmetry quality | PR |  |  |  |  |  |  |  |
| Symmetry |  |  |  |  |  |  |  |  |
| Polish |  |  |  |  |  |  |  |  |
| Color |  |  |  |  |  |  |  |  |
|  |  |  |  |  |  | Girdle center |  | Culet center |  | Тable center |  |  | Paint / Dug | Avg | Max | Type |
| Clarity |  |  |  | Offset by table axis |  |  | Crown, ° | -1.59 | -4.13 | Painting |
|  |  |  |  | Girdle-Culet | 1.50 ± 0.26, % | 0.072 ± 0.012, mm |  |  | Crown, notches | 0.4, Small | 1.1 |  |
| Fluorescence |  |  |  | Girdle-Table | 1.28 ± 0.23, % | 0.061 ± 0.011, mm |  |  | Pavilion, ° | -0.28 | -1.92 |  |
|  |  |  |  | Table-Culet | 1.82 ± 0.27, % | 0.087 ± 0.013, mm |  |  | Pavilion, notches | 0.1, Absent | 0.5 |  |