| HELIUM ILLUSTRATED REPORT |  |  | Parameter | Avg | Min | Max | Dev | Cut | Sym |  |  | 1 | 2 | 3 | 4 | 5 | 6 | 7 | 8 |
| --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- |
| Polished Brilliant |  |  |  | Diameter, mm | 6.705 | 6.692 | 6.717 | 0.37% | N/A | EX |  |  | 6.715 | 6.698 | 6.716 | 6.698 |  |  |  |  |
|  |  |  |  | Crown angle, ° | 34.70 | 34.49 | 34.82 | 0.33 | E-VG | EX |  |  | 34.77 | 34.82 | 34.74 | 34.58 | 34.49 | 34.67 | 34.73 | 34.81 |
|  |  |  |  | Pavilion angle, ° | 41.30 | 41.17 | 41.49 | 0.32 | N/A | EX |  |  | 41.17 | 41.35 | 41.49 | 41.31 | 41.34 | 41.27 | 41.23 | 41.20 |
| Model | Gauge |  |  | Total height, % | 61.51 |  |  |  | N/A | - |  |  |  |  |  |  |  |  |  |  |
| Expert name | N/A |  |  | Crown height, % | 14.83 | 14.69 | 15.03 | 0.35 | N/A | EX |  |  | 15.03 | 14.88 | 14.85 | 14.69 | 14.77 | 14.70 | 14.88 | 14.89 |
| Report date | 23.05.2006 |  |  | Pavilion depth, % | 43.33 | 43.07 | 43.57 | 0.50 | E-VG | EX |  |  | 43.07 | 43.25 | 43.57 | 43.43 | 43.57 | 43.31 | 43.27 | 43.21 |
| Real weight, ct |  |  |  | Table, % | 57.12 | 56.99 | 57.21 | 0.22 | E-VG | EX |  |  | 56.99 | 57.18 | 57.21 | 57.09 |  |  |  |  |
| Calculated weight, ct | 1.14, 1.1423 |  |  | Upper girdle angle, ° | 40.24 | 39.81 | 40.74 | 0.93 | - | EX |  |  | 40.74 | 40.56 | 40.27 | 40.24 | 39.99 | 39.94 | 39.94 | 40.07 |
| Spread | -0.02 ct, -2.08% |  |  |  |  |  |  |  |  |  |  |  | 39.81 | 40.14 | 40.25 | 40.28 | 40.33 | 40.40 | 40.50 | 40.40 |
| Measurements, mm | 6.705 (6.692-6.717) x 4.124 /0.003 |  |  | Star angle, ° | 21.95 | 21.65 | 22.34 | 0.69 | - | EX |  |  | 22.17 | 21.83 | 21.90 | 21.85 | 21.65 | 21.75 | 22.13 | 22.34 |
|  |  |  |  | Lower girdle angle / Halves angle, ° | 42.47 | 42.20 | 42.73 | 0.53 | - | EX |  |  | 42.36 | 42.45 | 42.53 | 42.59 | 42.73 | 42.62 | 42.44 | 42.44 |
| Average values, mm |  |  |  |  |  |  |  |  |  |  |  | 42.59 | 42.62 | 42.38 | 42.42 | 42.44 | 42.45 | 42.27 | 42.20 |
| Crown height | Pavilion depth | Table | Culet | Girdle |  |  | Star: | 52.17: | 50.48: | 53.42: | 2.93 | - | - |  |  | 53.36: | 51.81: | 52.79: | 50.48: | 52.04: | 52.57: | 53.42: | 50.88: |
|  |  |  |  | Bezel | Bone | Valley |  |  | Upper ratio, % | 47.83 | 49.52 | 46.58 |  |  |  |  |  | 46.64 | 48.19 | 47.21 | 49.52 | 47.96 | 47.43 | 46.58 | 49.12 |
| 0.995 | 2.906 | 3.830 | 0.111 | 0.219 | 0.264 | 0.137 |  |  | Culet, % | 1.65 | 1.46 | 1.76 | 0.30 | N/A | EX |  |  |  |  |  |  |  |  |  |  |
|  |  |  |  |  |  |  |  |  | Twist, ° | 0.44 | 0.00 | 0.81 | 0.81 | - | EX |  |  | 0.81 | 0.21 | 0.41 | 0.62 | 0.80 | 0.54 | 0.00 | 0.11 |
|  |  |  | Girdle Bezel, % | 3.27 | 3.09 | 3.43 | 0.33 | G | EX |  |  | 3.43 | 3.23 | 3.09 | 3.33 | 3.17 | 3.33 | 3.33 | 3.24 |
|  |  |  |  | Girdle Bone, % | 3.94 | 3.82 | 4.07 | 0.25 | - | EX |  |  | 4.07 | 3.93 | 3.82 | 3.94 | 3.87 | 4.01 | 3.98 | 3.85 |
|  |  |  |  | Girdle Valley, % | 2.04 | 1.72 | 2.22 | 0.50 | N/A | EX |  |  | 2.00 | 2.11 | 2.10 | 1.97 | 1.72 | 2.04 | 2.21 | 1.96 |
|  |  |  |  |  |  |  |  |  |  |  |  |  | 1.92 | 2.00 | 2.22 | 2.06 | 2.01 | 2.11 | 2.10 | 2.14 |
|  |  |  |  | Total height, mm | 4.124 |  |  |  | N/A | - |  |  |  |  |  |  |  |  |  |  |
|  |  |  |  | Crown height, mm | 0.995 | 0.985 | 1.008 | 0.023 | - | - |  |  | 1.008 | 0.997 | 0.995 | 0.985 | 0.990 | 0.985 | 0.997 | 0.998 |
|  |  |  |  | Pavilion depth, mm | 2.906 | 2.888 | 2.922 | 0.034 | - | - |  |  | 2.888 | 2.900 | 2.922 | 2.912 | 2.921 | 2.904 | 2.901 | 2.897 |
|  |  |  |  | Table, mm | 3.830 | 3.821 | 3.836 | 0.015 | - | - |  |  | 3.821 | 3.834 | 3.836 | 3.828 |  |  |  |  |
|  |  |  |  | Culet, mm | 0.111 | 0.098 | 0.118 | 0.020 | - | - |  |  |  |  |  |  |  |  |  |  |
|  |  |  |  | Girdle Bezel, mm | 0.219 | 0.207 | 0.230 | 0.022 | - | - |  |  | 0.230 | 0.217 | 0.207 | 0.223 | 0.213 | 0.223 | 0.223 | 0.217 |
|  |  |  |  | Girdle Bone, mm | 0.264 | 0.256 | 0.273 | 0.017 | - | - |  |  | 0.273 | 0.263 | 0.256 | 0.264 | 0.260 | 0.269 | 0.267 | 0.258 |
|  |  |  |  | Girdle Valley, mm | 0.137 | 0.115 | 0.149 | 0.034 | - | - |  |  | 0.134 | 0.141 | 0.141 | 0.132 | 0.115 | 0.137 | 0.148 | 0.131 |
|  |  |  |  |  |  |  |  |  |  |  |  |  | 0.128 | 0.134 | 0.149 | 0.138 | 0.135 | 0.141 | 0.141 | 0.143 |
|  |  |  |  | Measurement as per OctoNus theory: |  |  |  |
|  |  |  |  | Crown angle, ° | 34.70 | 34.63 | 34.75 | 0.11 | - | - |  |  | 34.63 | 34.75 | 34.74 | 34.69 |  |  |  |  |
|  |  |  |  | Pavilion angle, ° | 41.30 | 41.25 | 41.36 | 0.11 | - | - |  |  | 41.25 | 41.31 | 41.36 | 41.25 |  |  |  |  |
|  |  |  |  | Fish eye effect, ° | 10.11 | N/A |  |  |  | Extra Facet / Nat | No |
|  |  |  |  | Culet through Crown Bezel, ° | 10.35 | N/A |  |  |  | Girdle to MIC, mm | 0.003 |
|  |  |  |  | Azimuths deviation from ideal | 1 | 2 | 3 | 4 | 5 | 6 | 7 | 8 |  |  |  |
|  |  |  |  | Pavilion, ° | 0.00 | -0.46 | -0.16 | 0.14 | 0.31 | 0.46 | 0.40 | 0.35 |  |  |  |
|  |  |  |  | Lower girdle facets / Pavilion Halves, ° | -0.35 | -0.11 | -0.53 | -0.31 | -0.31 | -0.28 | -0.07 | 0.33 |  |  |  |
|  |  |  |  |  | 0.17 | 0.45 | 0.60 | 0.61 | 0.80 | 0.75 | 0.11 | 0.04 |  |  |  |
|  |  |  |  | Crown, ° | -0.81 | -0.67 | -0.57 | -0.48 | -0.49 | -0.08 | 0.39 | 0.46 |  |  |  |
|  |  |  |  | Upper girdle facets, ° | -2.76 | 2.31 | -2.40 | 1.43 | -3.46 | 2.03 | -2.96 | 1.59 |  |  |  |
|  |  |  |  |  | -2.71 | 2.07 | -2.71 | 2.57 | -2.14 | 2.53 | -1.55 | 0.95 |  |  |  |
|  |  |  |  | Star facets, ° | -0.25 | -0.67 | -0.32 | -0.20 | -0.43 | 0.80 | 0.96 | 0.43 |  |  |  |
| Appraiser title | GIA |  |  |  |  |  |  |  |
| Overall cut quality | G |  |  |  |  |  |  |  |
| Overall symmetry quality | GD |  |  |  |  |  |  |  |
| Symmetry |  |  |  |  |  |  |  |  |
| Polish |  |  |  |  |  |  |  |  |
| Color |  |  |  |  |  |  |  |  |
|  |  |  |  |  | Girdle center |  | Culet center |  | Тable center |  |  |  |
| Clarity |  |  |  | Girdle-Culet offset (by table axis) | Girdle-Table Offset (by table axis) | Table-Culet Offset (by table axis) |  |  | Girdle type | Digging (Gouging) |
| Fluorescence |  |  |  | 0.28 ± 0.20, % | 0.21 ± 0.17, % | 0.25 ± 0.21, % |  |  |  | -0.67, % |
|  |  |  |  | 0.019 ± 0.013, mm | 0.014 ± 0.012, mm | 0.017 ± 0.014, mm |  |  |  | -0.045, mm |